| Litiz LTD | Control Chart of Casting Parts |
| --- | --- |
|  | Capot |
| CC № 35 Rev. 0 Date Page № 1 Pages 25__ |
| Developed by: V. Polyakov. | Confirmed by: А. Klochko | Verified by: A. Astafyev, D. Podolyan |
| Material: | Alloy EN 47100 EN 1676 |
| Operation: | Control |
| General information. These instructions are intended for the supervisors of the technical control department and determine the order and plan for inspection of the part “Nano 2 Capot” after the technical operations of “Drilling,” and “Packing.” Goods are provided for control by batches. Batch of goods: A quantity of parts made during one labor shift, produced from a single piece of equipment and one operator, and then placed in a single multiway container. Each batch of goods is given for inspection to the department foreman of the technical control department after he personally makes sure the parts meet the requirements of all the regulatory documents. Each batch of goods must be identified by an itinerary sheet with the description of the goods, date of manufacturing, surname of the production worker (or shift number) along with the machine operator’s signature. The part “Nano 2 Capot” is under control in accordance with the requirements of “PQ Sheet Nano-2 Capot,” rev. А. developed 10th July, 2012 by the Schréder company in accordance to Annex № 5 to the Supply Contract. Monitoring requirements. Monitoring of parts after the technical operation of “Drilling.” Table 1. Batch quantity, pcs. Amount produced: pcs. Acceptance number: pcs. Non-conformity number: pcs. 51 – 90 5 0 1 91 – 150 8 0 1 151 – 280 13 0 1 281 – 500 20 1 2 501 – 1200 32 1 2 |

| Litiz LTD | Control Chart of Casting Parts |
| --- | --- |
|  | Capot |
| CC № __35_ Rev. 0 Page № 2 Pages 25__ |
| The visual appearance of the part after the “Drilling” operation should correspond to image №1-5. Inspection – complete. Method – visual inspection. Image 1. |

| Litiz LTD | Control Chart of Casting Parts |
| --- | --- |
|  | Capot |
| CC № __35_ Rev. 0 Page № 3 Pages 25__ |
| Image 2. |
| Litiz LTD | Control Chart of Casting Parts |
|  | Capot |
| CC № __35_ Rev. 0 Page № 4 Pages 25__ |
| Image 3 |
| Litiz LTD | Control Chart of Casting Parts |
|  | Capot |
| CC № __35_ Rev. 0 Page № 5 Pages 25__ |
| Image 4 |
| Litiz LTD | Control Chart of Casting Parts |
|  | Capot |
| CC № __35_ Rev. 0 Page № 6 Pages 25__ |
| Image 5 |

| Litiz LTD | Control Chart of Casting Parts |
| --- | --- |
|  | Capot |
| CC № __35_ Rev. 0 Page № 7 Pages 25__ |
| Monitoring of casting quality and absence of unacceptable or uncorrected foundry defects: Requirements for the quality of castings is in accordance to the CC № 31, “Control Chart” of Casting Parts, “Nano 2 Capot (Trimming).” Additionally on the processed surface, holes up to 0.5 mm in diameter and pinholes (gas bubbles) no greater than 0.75 mm are permitted. Inspection – complete. Method – visual inspection. The part should be cleaned and all burrs and strews removed. Burrs should be cleaned flush with the surface of the part. Sharp edges and burrs must be removed by grinding. Surface defects must be removed (image 6 – 14). Inspection – complete. Method – visual inspection. Image 6 |

| Litiz LTD | Control Chart of Casting Parts |
| --- | --- |
|  | Capot |
| CC № __35_ Rev. 0 Page № 8 Pages 25__ |
| Image 7 |

| Litiz LTD | Control Chart of Casting Parts |
| --- | --- |
|  | Capot |
| CC № __35_ Rev. 0 Page № 9 Pages 25__ |
| Image 8 |

| Litiz LTD | Control Chart of Casting Parts |
| --- | --- |
|  | Capot |
| CC № __35_ Rev. 0 Page № 10 Pages 25__ |
| Image 14 |

| Litiz LTD | Control Chart of Casting Parts |
| --- | --- |
|  | Capot |
| CC № __35_ Rev. 0 Page № 11 Pages 25__ |
| Control of bore diameter Ø15.5 mm. Control by caliper -I-125-0.05 (image 15, 16). Inspection - selective. Acceptable quality level (AQL) 1.5, inspection level I. The sample size, acceptance and rejection number is dependent on the batch specified in the Table. Image 15 |

| Litiz LTD | Control Chart of Casting Parts |
| --- | --- |
|  | Capot |
| CC № __35_ Rev. 0 Page № 12 Pages 25__ |
| Image 16 |

| Litiz LTD | Control Chart of Casting Parts |
| --- | --- |
|  | Capot |
| CC № __35_ Rev. 0 Page № 13 Pages 25__ |
| Monitor the availability and quality of М8 thread in holes for luminaire mounting (images 17 – 21). Thread quality control - selective. Method of inspection – by plug gauge. Thread availability control – one hundred percent inspection. Method – visual inspection. Image 17 |

| Litiz LTD | Control Chart of Casting Parts |
| --- | --- |
|  | Capot |
| CC № __35_ Rev. 0 Page № 14 Pages 25__ |
| Image 19 |

| Litiz LTD | Control Chart of Casting Parts |
| --- | --- |
|  | Capot |
| CC № __35_ Rev. 0 Page № 15 Pages 25__ |
| Image 20 |

| Litiz LTD | Control Chart of Casting Parts |
| --- | --- |
|  | Capot |
| CC № __35_ Rev. 0 Page № 16 Pages 25__ |
| Image 23 |

# Text boxes

PAY PARTICULAR ATTENTION

PAY PARTICULAR ATTENTION

PAY PARTICULAR ATTENTION

PAY PARTICULAR ATTENTION

Controlled bore

Bore diameter measurement

Holes with М8 thread

During the control procedure, the part of plug gauge “Go” should enter into a thread freely and completely without effort (up to the end of the threaded part of the caliber)

During the control the part of the procedure, the plug gauge “Ngo” should not enter into the thread more than 2.5 turns